**A close up of a sign

Description generated with very high confidence**

**CENTRALLY CONNECTED VERTICAL RADIATOR**

**Material & surface:**

Made of cold-rolled steel sheet according to EN 442-1, stable, shapely profiling with 50 mm bead pitch, base coating In accordance with DIN 55900 Part 1, baked at 190°C, pre-painted with an electrostatic powder coating according to DIN 55900 Part 2, in RAL 9016, firing at 210°C object temperature

**Installation:**

The PLAN VERTICAL RADIATOR has a total of 6 G 1/2 "connections. Advantageously, the connection via the standard centre connection (50 mm). If the side (bottom) connections are used, the connection is made from underneath. Suitable valve connection fitting for central connection (see accessories). Other connection types are not recommended.

Performance tested in accordance with DIN EN 442 and permanently monitored in accordance with EN-ISO 9001 triple packaged (cardboard box, edge protection, shrink film).

The scope of delivery of PLAN VERTICAL RADIATOR includes wall rails with appropriate screws and dowels. For easier installation, the radiator is supplied with a corresponding drilling template. The recommended minimum distance to the ground of 150 mm should be maintained.

**Sizes**

* Connections - Centre connection, 6 x 1/2 "
* Lengths - 300, 450, 600 and 750 mm
* Heights – 1500, 1800, 1950, 2100 and 2300mm
* Types – 10, 20, 21 and 22

A close up of a sign

Description generated with high confidence